This is some documentation about Iradina CODE.

This documentation is additional to the original documentation on the Iradina code.

Help on the GUI can be found from the GUI itself by clicking on the blue button with a question mark.

Help about installing the GUI on windows or linux can be found in files Installation_Windows.txt or README_Linux.txt respectively

How to calculate energy loss

Using store_energy_deposit=1 (and normalize_output=0) one can calculate either the global energy loss or the ion energy loss of an irradiation

With Full cascade or KP calculations (see below), *.energy.electronic and *.energy.phonons stores the energy lost in the cells by the ion AND the secondary knocked-on atoms. For the secondary atoms, the energy lost in either calculated (Full cascade case) or estimated by Robinson Formula (KP case).  The Full Cascade option is naturally more accurate.

With simulation_type==3 (ion trajectory only), only the energy loss experienced by the ion is stored. *.energy.electronic and *.energy.phonons are then the energy lost by the ION only through electronic and BALLISTIC processes.

CAVEAT :

The sum in all cells of the energy losses is NOT equal to the initial energy of the ions ! Indeed some moving ions are retro-diffused out of the sample. Thus some energy is not lost in the sample. Only with a calculation “from inside the bulk” (ion_distribution=4) and a large enough box, one obtains that the sum of all energy losses is equal to the energy of the ions.

How to do SRIM-like calculations

You can do SRIM like calculations on homogenous materials with Iradina_GUI. If you want to do it directly with Iradina (e.g. for complex structures), you have to follow the following rules :

Options in the input file:

scattering_calculation=0 is mandatory to have scattering “à la corteo” ;

transport_type=1 is mandatory to ensure fast transport type (transport_type=0 does not work for KP calculations and has not been compared to SRIM for the Full Cascade calculations

normalize_input=1 is preferred as the ouputs are normalized in cm-1.

There are three types of possible calculations

“Full Cascade”, “KP” and “ion distribution only”

To reproduce SRIM Full Cascade calculations:

flight_length_type =0. This sets on the standard Poisson distributed flight length and impact parameters

simulation_type==0. This sets on Full Cascade calculations, i.e. the ions and all the knocked-on atoms are described.

To reproduce SRIM KP calculations (see below for technical details):

flight_length_type =3 . This sets on SRIM like free flight paths.

simulation_type==4. This sets on the KP calculation of damage.

To simply follow the ion trajectory set

To reproduce SRIM Full Cascade calculations:

flight_length_type =0. This sets on the standard Poisson distributed flight length and impact parameters

simulation_type==3. This sets makes the code follow the ion only without any estimation of damage.

Changes of the code with respect to Jena’s version :

CEA’s version of the code may be slightly different from Jena’s version by C. Borschel and C. Ronning. The source code used in the GUI can be found in iradinaGUI\iradinaCodes\iradina_cea.

The major change relates to the value of the minimum energy of moving atoms. In Jena’s original version, this energy is set to the lattice energy of the atoms (Elatt, around 4eV). In CEA’s version this energy is set to the threshold displacement energy (Ed around 40eV).

New possible value of the input variable store_range3d. store_range3d=2 stores not only the positions of the implanted ions but also the positions of each interstitials and vacancies for each cascade in *.ions.range3dI and *.ions.range3dV respectively. WARNING : this option creates rapidly very big files. It should be used only with small numbers of ions (max_no_ions).

New possible value of the input variable ion_distribution. ion_distribution pilots the entry positions of the ions. The new value ion_distribution=4 makes the ions starts from inside the material. Precisely the cascade is initiated at the center of the box. This options allows to describe internal irradiations such as alpha decay or neutron accelerated PKAs.